370       	TRADITIONAL ALUMINIUM PIPEWORK FOR EXTERNAL USE:

Manufacturer: Marley Alutec, Unit 1 (G-H), Hudson Road,
Elms Farm Industrial Estate, Bedford MK41 0LZ
Tel: 01234 359438, Fax: 01234 357199.
Email: enquiries@marleyalutec.co.uk

Reference: Tudor square aluminium rainwater system to BS8530.

Accessories: Bends, Branches, Access Pipes, 2 Piece Offset, Shoes, Hopper Head, Pipe Clips
Size: 102mmØ 
Type / grade: Marine Grade extruded aluminium to BS EN755-2:2008 grade 6063-T5 pipe

with cast aluminium sockets to BS EN 1706:2010

Finish: Polyester powder coated to BS EN 12206-1:2004

Colour: TBC

Functional life expectancy: 50 years

Fixing: Via eared cast sockets and or extruded pipe clips. Plug and screw to wall with Alutec M6 x 70mm hex. coach screw

Jointing: Cast sockets, sealed with Alutec sealant allowing for a 3-4mm vertical thermal movement gap