370       	VANDAL SQUARE ALUMINIUM PIPEWORK FOR EXTERNAL USE:

Manufacturer: Marley Alutec, Unit 1 (G-H), Hudson Road,

Elms Farm Industrial Estate, Bedford MK41 0LZ
	Tel: 01234 359438, Fax: 01234 357199.
	Email: enquiries@marleyalutec.co.uk

Reference: Vandal square aluminium rainwater system.

Accessories: Bends, Branches, Access Pipes, 2 Piece Offset, Shoes, Hopper Head
Size: 72x72mm 
Type / grade: Marine Grade extruded aluminium to BS EN755-2:2008 grade 6063-T5 pipe

Finish: Polyester powder coated to BS EN 12206-1:2004

Colour: TBC
	Functional life expectancy: 50 years

Fixing: Via concealed fixing plates. Plug and screw to wall with Alutec 50mm x No. 12 countersunk screws

Jointing: Internal spigot jointing, joints to be sealed with Alutec sealant allowing for a 3-4 mm vertical thermal movement gap