311         EVOLVE ALUMINIUM GUTTERS

	Manufacturer: Marley Alutec, Unit 1 (G-H), Hudson Road,
	Elms Farm Industrial Estate, Bedford MK41 0LZ
	Tel: 01234 359438, Fax: 01234 357199.
	Email: enquiries@marleyalutec.co.uk
	Reference: Evolve Half Round aluminium rainwater system
	Profile: Half Round
	Size: 123x51mm 
Flow Performance: 1.8 litres per second (centre outlet).

Outlet Size: 63mmØ or 76mmØ TBC
	Type / grade: Marine grade extruded aluminium to BS EN 755-2:2008

Finish:  Polyester powder coated to BS EN 12206-1:2004 
	Colour: TBC

Functional life expectancy: 50 years

Jointing: External JuraJoint joint union with integral EPDM rubber and cross linked with Alutec sealant

Fixing: BS EN 1462:2004 Class H, external fascia brackets at 1m centres. Fixed with Alutec austenitic stainless steel 32mm x No. 10 round head screws